WOODGRAINING MADE SIMPLE

By Paul Dobbin

Henry Ford knew that woodgrained instrument panels and window moldings in automobiles gave the motorcar a richer more luxurious look and feel.  The "Deluxe" had wood graining and a little extra exterior trim and a higher price.  The wood graining obviously made the car last much longer.  Look around at all the "deluxe" restored cars at shows, very few "standard" models survived.  Now look inside, many of those "deluxe" cars have "standard" dashes and moldings, all painted.   You can fix that yourself !

NOW YOU CAN LEARN THE ART OF WOODGRAINING IN 10 MINUTES

1.  Remove all the pieces to be wood grained.  It's best to do them all at the same time so they will look like they came from the same tree. (At least the same kind of wood)

2.  Before you strip and repair the pieces, look for the original base color on the back of the piece.  If you want the original look, have this color matched. Other wise pick you own base color.  Remember the darker the base color, the darker the finished piece will be.

(Red oxide primer makes a good base for cherry or walnut grain finishes)

3.  Strip and repair all pieces and paint with you base color, making sure to paint all sides, top and bottom.  Urethane base color can eliminate the need for sanding before applying the grain.  The lighter the base color, the more the graining shows.

4.  Gather your graining stuff to a work area where you can hang you finished pieces to dry.

ITEMS NEEDED:

A.   Rubber base printers ink (Yep the original stuff) Use brown unless you need red

grain for cherry or redwood.  I use Vandijk Brown Ink by Van Son Holland Ink.

B.   Press wash (ink solvent)

C.   Latex gloves or rubber gloves (ink will give you horrible hand stains)

D.   A coarse sponge, a 2 inch fine soft bristle paint brush, cheese cloth, Q-tips.

E.   A couple saucers or shallow bowls or plates.

F.   A photo of the original wood grain or a piece of wood that looks like what you

want.  Remember beauty is in the eye of the beholder and you beholden it.                 5.  Now the fun begins!!!   Pour a little press was into a shallow dish (just a little)

Dip the cheesecloth or sponge in the press wash then into the ink and apply to the painted areas.  If it runs it’s to wet if it globs up it's to dry.  Practice makes perfect.  Practice on a painted sheet of metal.  If you don't like it wipe it off as you apply, try again, it's very forgiving.  It’s like finger painting when you were a kid, you paint until you like the way it looks!

TRICKS OF THE MASTERS:

A. Wood has more than one directional grain so you can do that too.  Dab on the ink with a sponge or cheese cloth, then use the use the sponge or cheesecloth to add the long grain over it, being careful not to wipe all the cross grain off. Then use the paintbrush to blend the two.

B.  Small sponge balls held with tweezers or Q-tips make knurled wood when dabbed/twisted. C. Once you develop your pattern, move on to the other pieces and do them in the same style. D. Don't forget to do around the edges, remember the edges are what you see when you look into the car through the window.

6.   Allow all this creativity to air dry for 24-48 hours while the press wash evaporates, leaving only the lush wood grain ink.  At this point you must lock in your creativity or change it.

7.   Spray all pieces with acrylic urethane clear with a wet look / hardener for the shine.

8.  Allow to dry in a dust free area.  Then re-install your deluxe wood grained pieces.

all of the materials necessary to wood grain a single car cost less than $30.00 and will be a clubs lifetime supply of wood graining materials.   Share you expertise and supplies.

9.  Take the money you saved by doing it yourself and go on a tour with your old car club.